Off-specular Mössbauer Reflectometry

L. Deáka, H. Spieringb, L. Bottyána, D.L. Nagya

aKFKI Research Institute for Particle and Nuclear Physics, Budapest, Hungary

bInstitute für Anorganische und Analytische Chemie, Johannes Gutenberg Universität,

## Mainz, Germany

Synchrotron Mössbauer Reflectometry (SMR), the grazing incidence nuclear resonant scattering of synchrotron radiation, can be applied to perform depth-selective phase analysis and to determine the isotopic and magnetic structure of thin films and multilayer. Off-specular SMR provides information from the lateral structure of multilayer. A theoretical approach of off-specular SMR is presented.

1. Introduction

The specularly reflected radiation from layered systems does not depend on the lateral structure; it depends only on the lateral averages of material parameters []. For studying lateral inhomogenities, such as magnetic domains etc., off-specular reflectometry is necessary. Domain structure of AF-coupled MLs is an issue of both theoretical and technological importance. Off-specular non-polarized [] and polarized neutron reflectometry [,], soft-x-ray resonant magnetic diffuse scattering [] and, very recently, off-specular Synchrotron Mössbauer Reflectometry (SMR) [] have been used to estimate the AF-domain-size distribution in magnetic MLs.

The theory of the off-specular neutron reflectometry based on the Distorted Wave Born Approximation (DWBA) [] has been published earlier [,,]. DWBA solves the problem of diffuse (off-specular) field as perturbation around the specular field, which latter field can be easily calculated, even for general stratified media, by suitable matrix methods [Error: Reference source not found,,,,]. In case of off-specular SMR the DWBA can also be applied and similarly the solution of the specular problem is well known in the literature [Error: Reference source not found,,,,,,,]. Because SMR works in the time domain, this approach is not straightforward. Our aim is the implementation of off-specular reflectometry into the data evaluation program EFFI (Environment For FItting) [].

Starting from the general theory of Lax [Error: Reference source not found] and from the common optical formalism of polarized neutron and Mössbauer reflectometry [Error: Reference source not found], an expression for diffuse scattering of multiple component (electromagnetic and/or quantum mechanical particle) waves on laterally inhomogeneous stratified media is obtained. As Lax has pointed out, from the point of view of specular reflection, the set of discrete atomic scattering centers can be described/replaced by homogeneous index of refraction n and solving the scattering problem is equivalent to solving the wave equation. This approach is valid only if the direction of the scattered wave is far from the direction of higher order atomic Bragg reflections. In this paper we study the grazing angle incidence limit only, for which the index of refraction approximation is valid [Error: Reference source not found,16,Error: Reference source not found].

Our model systems are stratified media, multilayer and thin films, having lateral inhomogeneity on the mesoscopic scale, being much larger then the atomic distances. In each homogeneous part around position r an index of refraction n(r) is defined. Since n for both slow neutrons and X-rays hardly differs from the 22 unit matrix I, the susceptibility defined by (r) = 2[n(r)-I] is conveniently used (see also Ref. [Error: Reference source not found]).

2. Off-specular scattering

Using the index of refraction approximation in each homogeneous part of the system the solution of the inhomogeneous wave equvation

Δ+k2IΨr=−k2χrΨr								(1)

yields (r), representing the two components of the electromagnetic field or the quantum mechanical spinor state of neutron at position r, with k being the wave number in vacuum. In stratified medium we compose the susceptibility function

χr=l=1SχlrII,									(2)

as the sum of the susceptibility functions of the individual layers l (l = 1..S, the last layer S is the substrate) depending on the lateral coordinate rII only.

If the homogeneous parts of the system are large compared to the wavelength, we may assume that the exact solution (r) is close to the solution Ψcohr of the coherent (specular) field equation

Δ+k2IΨcohr=−k2χlΨcohr,							(3)

which is obtained from Eq. (1) by replacing the susceptibilities χlrII by the average susceptibility χl=χlrII of each layer l [Error: Reference source not found]. In order to arrive at a perturbation equation, the sum −k2χlΨr is added and subtracted at the right hand side of Eq. (1)

Δ+k2IΨr=−k2χlΨr−k2χlrII−χlΨr.				(4)

For homogeneous layers χlrII=χl the second sum vanishes on the right, so that Eq. (4) is equivalent to Eq. (3), the basic equation of the specular reflectometry [Error: Reference source not found,Error: Reference source not found,Error: Reference source not found,Error: Reference source not found].

We look for the general solutions

Ψr=Ψcohr+Ψoffr								(5)

of Eq. (4) as the sum of the coherent field Ψcohr, which vanishes out of the specular direction, and the off-specular fieldΨoffr. Substituting Eq. (4) into Eq. (3) gives

Δ+k2IΨoffr=−k2χlrII−χlΨcohr−k2χlrIIΨoffr.			(6)

By the optical method [Error: Reference source not found] the coherent fieldΨcohr, the solution of Eq. (3), is obtained

Ψcohr=TrΨinexpikII⋅rII							(7)

(see Appendix), where r and rII are the perpendicular and lateral components of r, respectively and in the amplitude of the incident plane wave

Tr=L21rI−Rsp+L22rI+Rsp						(8)

is the transmission factor of the coherent field between the top surface r = 0 and an arbitrary depth r. Rsp is the 22 specular reflectivity matrix of the system [Error: Reference source not found], L[21](r) and L[22](r) are the 22 submatrices of the 44 characteristic matrix L at depth r [Error: Reference source not found,Error: Reference source not found].

Eq. (6) can be solved up to arbitrary accuracy applying higher order Born approximations. As our first approximation the second term of the right hand side is neglected, so the solution can be given by using the Green function technique

Ψoffr=k24πlexpikRRχlrII'−χlΨcohr'd3r',					(9)

where R=r−r'. The approximation requires Ψcohr>>Ψoffr, which condition is expected to be valid for magnetic domains in multilayer, where large enough homogeneous domains are observed [Error: Reference source not found,Error: Reference source not found], so that the exact solution Ψr is close to the coherent field Ψcohr according to the above condition.

Far from the scattering system the Fraunhofer approximation

expikRR≈expikrrexp−ik'⋅r'							(10)

is applied and the final result reads

Ψoffr=π2k2rexpikrlSlKIITlk'Ψin,					(11)

where

Tlk'=12πZlexp−ik'rTr dr						(12)

is the Fourier integral over the one dimensional interval Zl of layer l;

SlKII=12πexp−iKIIrIIχlrII−χld2rII					(13)

is the two dimensional Fourier transform of χlrII−χl and KII is the lateral component of the momentum transfer vector K = k’- k.

The off-specularly scattered intensity Ioff=Ψoff,Ψoff reads

Ioff=πk42r2ll'Ψin,Tl+k'Sl+KIISl'KIITl'k'⋅Ψin,				(14)

which for arbitrary incident polarization is written as

Ioff=πk42r2ll'TrTl+k'Sl+KIISl'KIITl'k'⋅ρ,					(15)

where  is the polarization density matrix of the incident radiation []. From the convolution theorem follows that the Fourier transform Cll'RII of

Cll'KII=12πSl+KIISl'KII,							(16)

is the cross correlation function of the susceptibilities between layers l and l’

Cll'RII=1AχlRII+rII−χl+χl'rII−χl'd2rII.				(17)

A is the area of the surface (A→∞). The final result then becomes

Ioff=πk42r2ll'TrTl+k'Cll'KIITl'k'⋅ρ,						(18)

which expression is very convenient in case of randomly distributed lateral inhomogenities.

3. Off-specular SMR

The result of Eq. (18) is valid for neutron and x-ray reflectometry working in the energy domain. However, in case of SMR we detect the time response after the synchrotron pulse [], which is

Ψoffr,t=1ℏ2π−∞∞Ψoffr,Eexp−iEtℏdE,					(19)

the Fourier transform of the off-specular field. As both the susceptibilities χlrII',E−χlE and the coherent field Ψcohr',E strongly depend on the energy E [Error: Reference source not found] and according to the definitions of Eqs. (8), (12) and (13), the energy dependence also regards to SlKII,E and Tlk',E, Eq. (18) can not been applied.

In order to work out Eq. (19) we define a geometric distribution function ΩlμrII of each homogeneous region  = 1,..,M in layer l. ΩlμrII describes the homogeneous area with an energy dependent susceptibility χlμE. Over the region of χlμE the distribution function ΩlμrII=1 otherwise ΩlμrII=0, so that the total inhomogeneous susceptibility is the sum

χr,E=μ=1Ml=1SΩlμrIIχlμE,							(20)

where the space and energy dependent parts of χr,E have been separated. The average susceptibility inside layer l reads

χlE=1Aμ=1MAlμχlμE,								(21)

where Alμ=ΩlμrIId2rII is the total area of the homogeneous part  inside layer l. Starting from Eqs. (13), (20) and (21)

SlKII,E=μ=1MGlμKIIχlμE,							(22)

with

GlμKII=12πexp−iKIIrIIΩlμrII−1AAlμd2rII,					(23)

we finally get the energy dependent off-specular field

Ψoffr,E=π2k2rexpikrl,μGlμKIIχlμETlk',EΨin				(24)

and the off-specular intensity

IoffE=k44r2ll'μμ'Cl'lμ'μKIITrΓl'μ'+k',EΓlμk',E⋅ρ.				(25)

The matrices for area , l

Γlμk',E=χlμETlk',E,								(26)

are the products of the homogeneous solution Tlk',E and the susceptibility χlμE of that area.

Cl'lμ'μKII=12πGl'μ'KIIGlμKII							(27)

is the geometrical correlation function between layers l and l’, homogeneous parts  and ’. In Eq. (25) the geometrical correlation function is separated from the energy dependent functions, and can therefore be applied for time domain and energy domain measurements, as well. Now the Fourier transformation can be worked out. With Eq. (19) the time dependent intensity becomes

Iofft=k44r2ll'μμ'Cl'lμ'μKIITrΓl'μ'+k',tΓlμk',t⋅ρ,				(28)

where

Γlμk',t=1ℏ2π−∞∞Γlμk',Eexp−iEtℏdE					(29)

4. Time integrated off-specular SMR

One possibility for off-specular reflectometry is the geometry called '-scan', where we set the value of 2  (we fix the height of the detector) and vary the sample orientation  (leaving the constraint of specular reflection  = ). In the special case of -scan the lateral components of the momentum transfer vector KII and the perpendicular component of the wave vector of the out coming wave k' can be expressed by the grazing angle  and by 

KII=2ksinθsinθ−ω								(30)

k'=ksinω.										(31)

The time-integrated intensity is Iω,θ=t1t2Iofftdt, where t1 and t2 define the time window of the measurements after the synchrotron bunch. Applying Eqs. (28) and (29) the final form reads

Iω,θ=NτtBunchk44ℏr2n=−∞∞Sn−∞∞dEll'μμ'Cl'lμ'μKIITrΓl'μ'+k',E+nℏΩ Γlμk',Eρ,	(32)

where N is the number of photons in the incident synchrotron bunch,  is the duration of the synchrotron bunch (50 ps at ESRF), tBunch is the time interval between the synchrotron bunches, Ω=2πtBunch and Sn are the discrete Fourier components of the periodical time window function St=n=−∞∞SnexpinΩt of the experiment defined by S(t)=1 for t1<t<t2, otherwise S(t)=0 after each synchrotron bunch.

5. Conclusion

Off-specular SMR is sensitive to the lateral structure of the hyperfine fields, so it can be used for studying magnetic domains in multilayer. Because of the underlying common optical approach the same theory can be applied for SMR, x-ray reflectometry, spin polarized neutron reflectometry [13] and x-ray resonance exchange scattering [,] for both specular and off-specular reflection. Using perturbation theory (DWBA), the off-specularly reflected intensity of SMR has been expressed by the geometrical correlation functions of the lateral structure and by the specular field profile in the layers. A newer version of the data evaluation computer program EFFI (Environment For FItting), based on this calculus, will be freely soon available [Error: Reference source not found,].

# Appendix

The solution of Eq. (3) was given in Refs. [Error: Reference source not found,Error: Reference source not found,Error: Reference source not found], where instead of the second order differential equation regarding to Ψcohr, after defining the derivative field Φr=iksinΘ−1Ψ'r, a system of first order differential equations was used [Error: Reference source not found]. The solution was given in terms of the 44 characteristic matrix L of the system [Error: Reference source not found,Error: Reference source not found,Error: Reference source not found]

ΦrΨr=Lr Φ0Ψ0,								(A1)

which equation has the physical meaning that there is linear connection between the fields in depth r = 0 and in arbitrary depth r the characteristic matrix L being the matrix coefficient. Taking into account the boundary conditions, the field at the top surfaces of the system (r = 0) is

Ψ0=Ψin+RspΨin,									(A2)

the sum , the incident in and the reflected Rspin waves so Eq. (A1) reads

ΦrΨr=Lr Ψin−RspΨinΨin+RspΨin,							(A3)

where the concept of impedance tensors was used [], taking into account that the fields at r = 0 are in vacuum (see Eqs. (21) and (22) of Ref. [Error: Reference source not found]). Expressing the second component from Eq. (A3), the field at arbitrary depth r reads

Ψr=L21rI−Rsp+L22rI+RspΨin,					(A4)

and using the notation Tr=L21rI−Rsp+L22rI+Rsp the solution of the three dimensional homogeneous wave equation is

Ψcohr=TrΨinexpikII⋅rII.							(A5)

# Acknowledgements

This work was partly supported by the Hungarian Scientific Research Fund (OTKA) under Contract No. T029409 and by the Hungarian Academy of Sciences (Contact No. AKP 2000-103 2,3). The financial support by the Deutscher Akademischer Austauschdienst (DAAD) is gratefully acknowledged.

[?] M. Lax, Rev. Mod. Phys. 23 (1951) 287.

[?] S. Langridge, J. Schmalian, C.H. Marrows, D.T. Dekadjevi and B.J. Hickey, Phys. Rev. Lett. 85 (2000) 4964.

[?] G.P. Felcher, Physica B 192 (1993) 137.

[?] V. Lauter-Pasyuk, H.J. Lauter, B. Toperverg, O. Nikonov, E. Kravtsov, M.A. Milyaev, L. Romashev and V. Ustinov, Physica B 283 (2000) 194.

[?] T.P.A. Hase, I. Pape, B.K. Tanner, H. Dürr, E. Dudzik, G. van der Laan, C.H. Marrows and B.J. Hickey, Phys. Rev. B 61 (2000) R3792.

[?] D.L. Nagy, L. Bottyán, B. Croonenborghs, L. Deák, B. Degroote, J. Dekoster, H.J. Lauter, V. Lauter-Pasyuk, O. Leupold, M. Major, J. Meersschaut, O. Nikonov, A. Petrenko, R. Rüffer, H. Spiering and E. Szilágyi, Phys. Rev. Lett. 88 (2002) 157202

[?] S.L. Sinha, E.B. Sirota, S. Garoff, H.B. Stanley, Phys. Rev B 38 (1988) 2297

[?] B.T. Toperverg, Physica B 297 (2001) 160; B.T. Toperverg, O. Nikonov, V. Lauter-Pasyuk, H.J. Lauter, Physica B 297 (2001) 169

[?] V. Lauter-Pasyuk at al., J. Magn. Magn. Mater. 226-230 (2001) 1694.

[?] A. Rühm, B.T. Toperverg, H. Dosch, Phys. Rev. B. 60 (1999) 16073.

[?] G.P. Felcher, R.O. Hilleke, R.K. Crawford, J. Haumann, R. Kleb, and G. Ostrowski, Rev. Sci. Instrumm 58 (1987) 609.

[?] L.G. Parratt, Phys. Rev. 95 (1954) 359.

[?] C.F. Majkrzak, Physica B 156&157 (1989) 619.

[?] L. Deák, L. Bottyán, D.L. Nagy, and H. Spiering, Physica B 297 (2001) 113.

[?] A.M. Afanas'ev and Yu. Kagan, Sov. Phys. JETP 21 (1965) 215.

[?] J.P. Hannon and G.T. Trammell, Phys. Rev. 186 (1969) 306.

[?] J.P. Hannon, G.T. Trammell, M. Mueller, E. Gerdau, R. Rüffer, and H. Winkler, Phys. Rev. B 32 (1985) 6363.

[?] S.M. Irkaev, M.A. Andreeva, V.G. Semenov, G.N. Belozerskii and O.V. Grishin, Nucl. Instrum. Methods B 74 (1993) 545.

[?] S.M. Irkaev, M.A. Andreeva, V.G. Semenov, G.N. Beloserskii, and O.V. Grishin, Nucl. Instrum. Methods B 74  (1993) 554.

[?] L. Deák, L. Bottyán, D.L. Nagy and H. Spiering, Phys. Rev. B. 53 (1996) 6158.

[?] R. Röhlsberger, Ph.D. thesis, University Hamburg, 1994.

[?] H. Spiering, L. Deák, and L. Bottyán, Hyp. Int. 125 (2000) 197.

[?] M. Blume and O.C. Kistner, Phys. Rev. 171 (1968) 417.

[?] G.T Trammell and J.P. Hannon, Phys. Rev B 18 (1979) 165.

[?] J.P. Hannon, G.T. Trammell, M. Blume, and Doon Gibs, Phys. Rev. Lett. 61 (1988) 1245.

[?] L. Deák et al., to be published (not yet implemented into our data evaluation program, EFFI)

[?] The computer program EFFI is available from ftp://iacgu7.chemie.uni-mainz.de/pub/effi

[?] G.M. Borzdov, L.M. Barskovskii, and V.I. Lavrukovich, Zh. Prikl. Spektrosk. 25 (1976) 526.